|  | CrystaLite, Inc. 3307 Cedar Street Everett, WA 98201 | 1-800-666-6065 www.CrystaLiteInc.com info@crystaliteinc.com | CSI Specification: |
| --- | --- | --- | --- |
|  |  |  | Corrugated Polycarbonate Roof Sheets |

08 45 00 – Translucent Wall and Roof Assemblies

08 84 00 – Plastic Glazing

### Job Name:

Description:

### GENERAL

  - SECTION INCLUDES

    - This section covers all work necessary to the inclusion of polycarbonate corrugated plastic glazing material as shown on drawings and specified herein.

  - RELATED SECTIONS

    - Section 08 45 00 – Translucent Wall and Roof Assemblies

    - Section 08 84 00 – Plastic Glazing

  - REFERENCE

    - American Standards and Test Methods

      - ASTM D 1667 - Standard Specification for Flexible Cellular Materials - (Closed-Cell Foam)

      - ASTM D 792 - Standard Test Methods for Density and Specific Gravity (Relative Density) of Plastics by Displacement

      - ASTM D 695 - Standard Test Method for Compressive Properties of Rigid Plastics

      - ASTM D 638 - Standard Test Method for Tensile Properties of Plastics

      - ASTM D 790 - Standard Test Methods for Flexural Properties of Unreinforced and Reinforced Plastics and Electrical Insulating Materials

      - ASTM D 1925 - Test Method for Yellowness Index of Plastics (Withdrawn 1995)

      - ASTM D 648 -  Standard Test Method for Deflection Temperature of Plastics Under Flexural Load in the Edgewise Position

  - DESIGN REQUIREMENTS

    - Performance Specifications

| Property | Test Method | Average Index |
| --- | --- | --- |
| Specific Gravity | ASTM D 792 | 1.20 +/= 5% |
| Tensile Strength | CNS 11335 | 551 kgf/cm2 |
| Elongation | CNS 11335 | 50% |
| Compressive Strength | ASTM D 695 | 830 kgf/cm2 |
| Modulus of Elasticity | ASTM D 638 | 345000 psi +/- 10% |
| Flexural Strength | ASTM D 790 | 950 kgf/cm2 |
| Yellowing Index | ASTM D 1925 | Below 3.0 |
| Light Transmittance | Wave Length 500 nm (UV/VIS) | 90% |
| UV-Ray Penetrability | WL 300 nm (UV/VIS) – 3 hrs | 2.4% |
| Impact Strength | CNS 113355 (1kg ball – 120 cm height) | Unbreakable |
| Inflammability | UL 94V2 | Self-Extinguishing |
| Deflection Temperature | ASTM D 648 (18.6 kgf/cm2) | 135°C |
| Brittle Temperature | ASTM D 764 | -135°C |

    - Recommended Loading

      - It is recommended that all rafter centers be no greater than 24”. Runs shall be supported by perlins a minimum of every 4 ft.

  - SUBMITTALS

    - Submit full scale shop drawings indicating methods of construction, location and spacing of anchorage, joinery, finishes, size, shape, thickness of framing members, relationship to adjoining work and glazing materials used.

    - Submit samples of each type of glazing material as required by architect.

  - DELIVERY, STORAGE, AND HANDLING

    - Deliver materials to site in manufacturer’s original and unopened packaging.

    - Store on site in a location and manner to avoid damage. Stacking should be done in a manner that will prevent damage. Store material in a clean, dry location away from high traffic areas. Any protection on the product during transportation should remain until installed.

    - Keep handling on site to a minimum.

### PRODUCTS

  - MANUFACTURER

    - Drawings and specifications are based on products manufactured by:

Amerilux International, LLC

DePere, WI 54115

Distributed by:

CrystaLite, Inc.

3307 Cedar Street

Everett, WA 98201

1-800-666-6065

www.crystaliteinc.com

    - Substitutions:  Not permitted.

  - MATERIALS

    - Polycarbonate multi-wall sheet. Color shall be (clear, bronze, white, other). Thickness as required by the span and loads. Fire Rating per application.

  - GLAZING ACCESSORIES

    - Glazing tapes per ASTM D 1667, 2240, 412, 925; ASTM C 518; NPT 11, 5, 57 Thermal Bond V 2100 high strength polyurethane foam substrate double sided tape. All other gaskets, setting blocks, and other materials used in glazing shall be of a type, quality and compatibility to provide performance of the product(s) covered in this section.

  - FABRICATION

    - Corrugated sheet(s) shall be field measured, cut, and assembled in accordance with manufacturer’s instructions.

### EXECUTION

  - INSTALLATION

    - Framing shall be installed and glazed by experienced workmen in accordance with the approved shop drawings, manufacturer’s instructions and glazing standards.

  - CLEANING AND PROTECTION

    - Subsequent to installation of product(s) the General Contractor shall be responsible for the cleanup and protection of all materials provided per this section, including, but not limited to glazing materials and framing members. No abrasive materials of any kind shall be used in cleaning of surfaces.